|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| **BRICK SIZE** | **APPROXIMATE WEIGHT** | **SIZE (INCHES) (Bed Depth X Height X Length)** | **MODULAR BRICK EQUIVALENT** | **UNITS PER SQ. FT. WALL (Inc. 3/8" Joint)** | **SIZE (MM)** | **METRIC UNITS/SQ M (w/10MM Joint)** |
| Modular Face Brick Dimensions | [MODULAR](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=modular) | 4.2 lbs. | 3-5/8" x 2-1/4" x 7-5/8" | 1 | 6.86 | 92 x 57 x 194 | 73.1 |
|  | | | | | | | |
| Standard Face Brick Dimensions | [STANDARD](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=standard) | 4.5 lbs. | 3-5/8" x 2-1/4" x 8" | 1.05 | 6.55 | 92 x 57 x 203 | 69.9 |
|  | | | | | | | |
| Jumbo Modular Face Brick Dimensions | [JUMBO MODULAR](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=jumbo+modular) | 5.1 lbs. | 3-5/8" x 2-3/4" x 7-5/8" | 1.22 | 5.76 | 92 x 70 x 194 | 61.3 |
|  | | | | | | | |
| Jumbo Standard Face Brick Dimensions | [JUMBO STANDARD](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=jumbo+standard) | 5.9 lbs. | 3-5/8" x 2-3/4" x 8" | 1.28 | 5.5 | 92 x 70 x 203 | 58.7 |
|  | | | | | | | |
| Plant 3 Jumbo Standard Face Brick Dimensions | [JUMBO STANDARD (PLT 3)](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=plant+3) | 5.6 lbs. | 3-5/8" x 2-5/8" x 8" | 1.28 | 5.73 | 92 x 67 x 203 | 61.2 |
|  | | | | | | | |
| Slim Jumbo Modular Face Brick Dimensions | [SLIM JUMBO MODULAR](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=slim+jumbo+modular) | 4.1 lbs. | 3-1/8" x 2-3/4" x 7-5/8" | 1.22 | 5.76 | 76 x 70 x 194 | 73.6 |
|  | | | | | | | |
| Queen Face Brick Dimensions | [QUEEN](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=queen) | 5.6 lbs. | 3-1/8" x 2-3/4" x 9-5/8" | 1.54 | 4.61 | 79 x 70 x 244 | 49.2 |
|  | | | | | | | |
| Roman Face Brick Dimensions | [ROMAN](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=roman) | 4.7 lbs. | 3-5/8" x 1-5/8" x 11-5/8" | 1.10 | 6.00 | 92 x 41 x 295 | 63.9 |
|  | | | | | | | |
| Norman Face Brick Dimensions | [NORMAN](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=norman) | 6.4 lbs. | 3-5/8" x 2-1/4" x 11-5/8" | 1.52 | 4.57 | 92 x 57 x 295 | 48.8 |
|  | | | | | | | |
| Jumbo Norman Face Brick Dimensions | [JUMBO NORMAN](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=jumbo+norman) | 7.8 lbs. | 3-5/8" x 2-3/4" x 11-5/8" | 1.86 | 3.84 | 92 x 70 x 295 | 41.0 |
|  | | | | | | | |
| Slim Jumbo Norman Face Brick Dimensions | [SLIM JUMBO NORMAN](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=slim+jumbo+norman) | 7.2 lbs. | 3-1/8" x 2-3/4" x 11-5/8" | 1.86 | 3.84 | 79 x 70 x 295 | 41.0 |
|  | | | | | | | |
| Modular Economo Face Brick Dimensions | [MODULAR ECONOMO](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=economo) | 6.8 lbs. | 3-5/8" x 3-5/8" x 7-5/8" | 1.61 | 4.50 | 92 x 92 x 194 | 48.1 |
|  | | | | | | | |
| Utility Face Brick Dimensions | [UTILITY](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=utility) | 10.2 lbs. | 3-5/8" x 3-5/8" x 11-5/8" | 2.46 | 3.00 | 92 x 92 x 295 | 32.1 |
|  | | | | | | | |
| Monarch Face Brick Dimensions | [MONARCH](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=monarch) | 12.5 lbs. | 3-5/8" x 3-5/8" x 15-5/8" | 3.30 | 2.25 | 92 x 92 x 397 | 24.1 |
|  | | | | | | | |
| Quad Face Brick Dimensions | [QUAD](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=quad) | 14.1 lbs. | 3-5/8" x 7-5/8" x 7-5/8" | 3.39 | 2.25 | 92 x 194 x 194 | 24.1 |
|  | | | | | | | |
| Ambassador Face Brick Dimensions | [AMBASSADOR](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=ambassador) | 8.8 lbs. | 3-5/8" x 2-1/4" x 15-5/8" | 2.05 | 3.43 | 92 x 57 x 397 | 36.6 |
|  | | | | | | | |
| Double Utility Face Brick Dimensions | [DOUBLE UTILITY](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=double+utility) | 21.0 lbs. | 3-5/8" x 7-5/8" x 11-5/8" | 5.17 | 1.50 | 92 x 194 x 295 | 16.1 |
|  | | | | | | | |
| Double Monarch Face Brick Dimensions | [DOUBLE MONARCH](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=double+monarch) | 25.5 lbs. | 3-5/8" x 7-5/8" x 15-5/8" | 6.94 | 1.13 | 92 x194 x 397 | 12.1 |
|  | | | | | | | |
| 6"x4"x16" Thru Wall Face Brick Dimensions | [6" x 4" x 16" THRU-WALL](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=thruwall) | 16.0 lbs. | 5-5/8" x 3-5/8" x 15-5/8" | 3.30 | 2.25 | 143 x 92 x 397 | 24.1 |
|  | | | | | | | |
| 8"x4"x16" Thru Wall Face Brick Dimensions | [8" x 4" x 16" THRU-WALL](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=thruwall) | 21.8 lbs. | 7-5/8" x 3-5/8" x 15-5/8" | 3.30 | 2.25 | 194 x 92 x 397 | 24.1 |
|  | | | | | | | |
| 8"x8"x16" Thru Wall Face Brick Dimensions | [8" x 8" x 16" THRU-WALL](https://www.beldenbrick.com/onlinecatalog/searchresults.aspx?search=thruwall) | 42.0 lbs. | 7-5/8" x 7-5/8" x 15-5/8" | 6.94 | 1.13 | 194 x 194 x 407 | 12.0 |